## Slide 1: Analysis of powder neutron diffraction data
The Rietveld method
Examples
MENA3100 – February 27 2017
Magnus H. Sørby

## Slide 2: Analysis of powder (neutron) powder diffraction data.
The Rietveld method
Introduced by Hugo Rietveld in 1967 H. M. Rietveld, Acta Cryst. 22 (1967) 151 H. M. Rietveld, J. App. Cryst. 2 (1969) 65
Revolutionized analysis of powder diffraction data. Cited times 11818. (10915 times 1 year ago)
Developed as a technique for structure refinement.

## Slide 3: The Rietveld method
Developed as a technique for structure refinement.
VD0.8
a = 3.16 Å
The pre-Rietveld life
hkl | Intensity
110 | 1000
200 | 82
211 | 80
220 | 120
310 | 285
.... | ....

## Slide 4: The Rietveld method
Developed as a technique for structure refinement.
Zr2NiD4.5 (300 oC)
a = 6.79 Å
c = 5.61 Å
The pre-Rietveld life
hkl | Intensity
101 | 23
110 | 34
002 | 10
121 | 120
112+220 | 450
022+130 | 1000
002
121
112/220
022/130

## Slide 5: The Rietveld method
Rietveld’s observations:
Well-resolved Bragg- peaks in his PND data had the shape of Gaussian curves.
The Gaussian curve

## Slide 6: The Rietveld method
Rietveld’s observations:
Well-resolved Bragg- peaks in his PND data had the shape of Gaussian curves.
The Gaussian curve

## Slide 7: The Rietveld method
Developed as a technique for structure refinement.
Zr2NiD4.5 (300 oC)
a = 6.79 Å
c = 5.61 Å
Rietveld’s idea:
Why not fit the entire calculated profile from the model to the data, instead of just the integrated intensities?
002
121
112/220
022/130

## Slide 8: The Rietveld method

## Slide 9: The Rietveld method

## Slide 10: The Rietveld method
The calculated profile
calculated intensity in point i

## Slide 11: The Rietveld method
The calculated profile
calculated intensity in point i
scale factor

## Slide 12: The Rietveld method
The calculated profile
calculated intensity in point i
scale factor
Sum over all Bragg peaks, K, that contribute with intensity to point i

## Slide 13: The Rietveld method
The calculated profile
calculated intensity in point i
scale factor
Lorentz factor and multiplicity
Sum over all Bragg peaks, K, that contribute with intensity to point i
= 1/(sin sin2) for powders

## Slide 14: The Rietveld method
The calculated profile
calculated intensity in point i
scale factor
Lorentz factor and multiplicity
The square modulus of the structure factor for Bragg peak K
Sum over all Bragg peaks, K, that contribute with intensity to point i

## Slide 15: The Rietveld method
The calculated profile
calculated intensity in point i
scale factor
Lorentz factor and multiplicity
The square modulus of the structure factor for Bragg peak K
Sum over all Bragg peaks, K, that contribute with intensity to point i
The profile function

## Slide 16: The Rietveld method
The calculated profile
calculated intensity in point i
scale factor
Lorentz factor and multiplicity
The square modulus of the structure factor for Bragg peak K
Sum over all Bragg peaks, K, that contribute with intensity to point i
The profile function
preferred orientation

## Slide 17: The Rietveld method
The calculated profile
calculated intensity in point i
scale factor
Lorentz factor and multiplicity
The square modulus of the structure factor for Bragg peak K
Sum over all Bragg peaks, K, that contribute with intensity to point i
The profile function
preferred orientation
absorption

## Slide 18: The Rietveld method
The calculated profile
calculated intensity in point i
scale factor
Lorentz factor and multiplicity
The square modulus of the structure factor for Bragg peak K
Sum over all Bragg peaks, K, that contribute with intensity to point i
The profile function
preferred orientation
absorption
background

## Slide 19: The Rietveld method
The parameters in yicalc undergo a least-square refinement to minimize Rwp
Fitting the profile

## Slide 20: The Rietveld method – structure refinement
The structure factor
The displacement factor
The square mean shift of the atom from its equilibrium position.

## Slide 21: The Rietveld method – structure refinement
The profile function
Gaussian:
Lorentzian:
pseudo-Voigt:

## Slide 22: The Rietveld method – structure refinement
An example
Approximate model of Al2O3:
  Trigonal, space group R –3 c
  a ~ 4.75 Å, c ~ 12.99 Å
  Al in 0 0 ~0.35 O in ~0.30 0 ¼
We want a more accurate structure model!
PND (PUS)

## Slide 23: Case: Th2AlD4
Very few metal hydrides with H-H distances below 2 Å are reported in the literature.
Th2AlD4 is a rare exception.

## Slide 24: Case: Th2AlD4
Very few metal hydrides with H-H distances below 2 Å are reported in the literature.
Th2AlD4 is a rare exception.
1.79 Å
Structure data (Bergsma et al. 1961)
a = 7.629 Å c = 6.517 Å s.g. I4/mcm
Th: 0.162 0.662 0
Al: 0 0 ¼
D: 0.368 0.868 0.137
D-D = 2*z(D)*c

## Slide 25: Case: Th2AlD4
PND anno 1961
PND today

## Slide 26: Case: Th2AlD4
X-ray diffraction

## Slide 27: Case: Th2AlD4
Neutron diffraction

## Slide 28: Conclusion
Rietveld refinement is an effective technique to refine crystal structure models against powder diffraction data.
It can also be used for quantitative phase analysis and to extract microstructural information.
The instrumental development has been great for the last decades.