## Slide 1: KJM 3110 Electrochemistry Chapter 14 Other interfaces
Most figures from the textbook we use for the course, via its web resources:

## Slide 2: Summary Ch. 13 The electrode interface
Interface
  Large capacitance
  Nonfaradaic currents
  Adsorption
  Next chapter: Other interfaces
ionic conductor
metal

## Slide 3: Metallic electrodes
So far:
  Working electrode is a metal (=is metallic (?))
  Always abundance of electrons
  Or rather: … of lectrons and states the electrons can be in.
Now, next:
  Working electrode is a semiconductor
  Not necessarily any longer an abundance of electrons. Or states.

## Slide 4: Semiconductor electrodes - overview
Semiconductor
  Lattice
  Valence band = HOMO
  Conduction band = LUMO
  Band gap
  Fermio energy (chemical potential of electrons)
  Work function (to bring electrons to vacuum)
n-type semiconductor
  Donor-doped n = [e-] = [D+]
  Electrons e- in the conduction band
p-type semiconductor
  Acceptor-doped p = [h+] = [A-]
  Electron holes h+ in the valence band

## Slide 5: n-type electrode – a closer look
Electroneutrality in the semiconductor bulk
n + [A-] = p + [D+]
Bulk donor doped n-type conductor
n ≈ [D+]
Adsorption of anions in Helmholtz layer
compensated by
positive space charge in the semiconductor
by
depletion of electrons
excess of holes
Band bending:
Cause: Adsorption of one of the ions (same as diffuse layer in the electrolyte)
Shape: Same origin (Poisson) as diffuse layer in the electrolyte
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+

## Slide 6: Exercise
How do the bands look before contact with the electrolyte?
Based on your memory and understanding, populate the top figure with ions, electrons, and holes
Populate the bottom figure with ions, electrons, and holes
How could we force the bands flat?
What is the flat-band potential?
Try to populate the valence bands with electrons instead of holes

## Slide 7: Photoelectrochemical (PEC) cell
n-type photoanode or p-type photocathode
Suitable bandgap
Charge separation
Photoanode

## Slide 8: PEC water splitting, artificial photosynthesis
Low efficiencies
Photocorrosion of electrodes
Cathode traditionally a noble (platinum group) metal
  Research: Non-noble metals, oxides. Enzymes
Sunlight cannot drive the reaction alone, just assist it
  Research: Combine photoanode and photocathode. Combine PV and PEC.
Reduce CO2 instead of H2O
Solid-state electrolyte instead of aqueous

## Slide 9: Artificial photosynthesis
Fujitsu Journal

## Slide 10: Interface between two immiscible electrolyte solutions (ITIES)
Aqueous vs organic liquids
Use of bipotentiostat

## Slide 11: Redox scales – SHE and ferrocene (C5H5)2Fe – for ITIES

## Slide 12: ITIES ion and electron transfers
Proton
Electron

## Slide 13: ITIES combined proton and electron transfers

## Slide 14: Phospholipid….
Zwitterion
Not curriculum

## Slide 15: Electrokinetic phenomena
Electrolyte – insulator interface
No electrical current across
But double layers form
Scales with interface area: Porous materials, suspensions, etc.
Silica:
  Terminating covalent O
  H2O adsorb
  Protolyses weakly (Silica is weakly acidic)
Glass
  Ionic alkali cations compenated by ionic terminating oxygen
  Reduces acidity
Adsorption of cations like Al3+ may reverse the charge

## Slide 16: Electroosmotic drag
Friction between the positive double layer and the solution volume
Volume rate v (m3/s)
Field X, radius R, viscosity η
Zeta potential ζ at the slip plane
  (zeta is ζ in the font set, not like in the formula in the textbook)
  Similar to Helmhotz potential φH
  Around -150 mV for glass, higher for silica
Electroosmotic flow is laminar, but it does not have the quadratic dependence of
velocity on radius, as described on pages 161162, that is seen in Poiseuille (laminar) flow. This is because electro-osmotic flow is not pressure-driven; instead, it is induced by friction from the motion of the field-driven sleeve. Thus the velocity profile is as shown in the Figure: it is uniform apart from within the narrow double-layer region.

## Slide 17: Electroosmotic drag
Electroosmotic flow by voltage or current
Electroosmotic pressure by voltage or current
Streaming potential or current by flow or pressure
Universality
Lars Onsager reciprocal relations
Irreversible thermodynamics
Nobel prize 1968
«Fourth law of thermodynamics»

## Slide 18: Ch. 14 Other interfaces - Summary